Online resource 1: XRD of synthesized (blue) and commercial (red) zeolite 4A.

Online resource 2: FT-IR spectra of adsorbed species formed by contact of CO2 at 298.15 K.

Online resource 3: FT-Raman spectra of adsorbed species formed by contact with CO2.

Online resource 4: FT-Raman spectra of adsorbed species formed by contact with H2S.

Online resource 5: FT-Raman spectra of adsorbed species formed by contact with CH4.

Online resource 6: Absolute and excess CO2 adsorption on zeolite 4A at 0.008, 25.009, 50.011 ºC

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 0.008 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.0274 | 3.3558 | ± | 0.0086 | 3.3564 |
| 0.1455 | 3.9710 | ± | 0.0100 | 3.9745 |
| 0.3902 | 4.3867 | ± | 0.0103 | 4.3960 |
| 0.7214 | 4.6510 | ± | 0.0154 | 4.6682 |
| 1.0933 | 4.8222 | ± | 0.0166 | 4.8483 |
| 1.4730 | 4.9429 | ± | 0.0203 | 4.9782 |
| 1.8409 | 5.0401 | ± | 0.0228 | 5.0843 |
| 2.1999 | 5.1117 | ± | 0.0258 | 5.1647 |
| 2.5292 | 5.1880 | ± | 0.0287 | 5.2491 |
| 2.8614 | 5.2269 | ± | 0.0313 | 5.2962 |
| 3.1642 | 5.2739 | ± | 0.0373 | 5.3507 |
| 3.4553 | 5.3074 | ± | 0.0379 | 5.3914 |
| 3.7324 | 5.3319 | ± | 0.0381 | 5.4228 |
| 3.9881 | 5.3596 | ± | 0.0440 | 5.4568 |
| 4.2258 | 5.3873 | ± | 0.0442 | 5.4906 |
| 4.4491 | 5.4118 | ± | 0.0497 | 5.5207 |
| 4.6664 | 5.4233 | ± | 0.0521 | 5.5377 |
| 4.8645 | 5.4407 | ± | 0.0519 | 5.5601 |
| 5.0525 | 5.4533 | ± | 0.0522 | 5.5775 |
| 5.2286 | 5.4651 | ± | 0.0557 | 5.5938 |
| 5.3936 | 5.4758 | ± | 0.0655 | 5.6087 |
| 5.5424 | 5.5016 | ± | 0.0622 | 5.6383 |
| 5.8941 | 5.5477 | ± | 0.0579 | 5.6935 |
| 6.2468 | 5.5563 | ± | 0.0606 | 5.7112 |
| 6.5675 | 5.5758 | ± | 0.0650 | 5.7390 |
| 6.8752 | 5.5821 | ± | 0.0657 | 5.7534 |
| 7.1526 | 5.6023 | ± | 0.0668 | 5.7809 |
| 7.4229 | 5.6051 | ± | 0.0756 | 5.7908 |
| 7.6653 | 5.6213 | ± | 0.0764 | 5.8135 |
| 7.8941 | 5.6333 | ± | 0.0785 | 5.8315 |
| 8.1166 | 5.6317 | ± | 0.0882 | 5.8358 |
| 8.3198 | 5.6367 | ± | 0.0878 | 5.8462 |
| 8.5289 | 5.6129 | ± | 0.0828 | 5.8281 |
| 8.7101 | 5.6109 | ± | 0.0951 | 5.8309 |

Online resource 6: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 0.008 ± 0.005 ºC |  |  |  |  |
| 8.8743 | 5.6164 | ± | 0.0984 | 5.8409 |
| 9.0300 | 5.6180 | ± | 0.0918 | 5.8467 |
| 9.1730 | 5.6230 | ± | 0.1010 | 5.8556 |
| 9.3033 | 5.6335 | ± | 0.1119 | 5.8697 |
| 9.4309 | 5.6346 | ± | 0.1187 | 5.8742 |
| 9.5480 | 5.6389 | ± | 0.1294 | 5.8817 |
| 9.6583 | 5.6419 | ± | 0.1320 | 5.8877 |
| 10.6985 | 5.6645 | ± | 0.1031 | 5.9391 |
| 11.3147 | 5.6707 | ± | 0.1073 | 5.9626 |
| 11.8926 | 5.6650 | ± | 0.1109 | 5.9732 |
| 12.4268 | 5.6629 | ± | 0.1155 | 5.9863 |
| 12.9189 | 5.6658 | ± | 0.1206 | 6.0036 |
| 13.3787 | 5.6640 | ± | 0.1256 | 6.0151 |
| 13.7956 | 5.6786 | ± | 0.1321 | 6.0420 |
| 14.1998 | 5.6654 | ± | 0.1374 | 6.0408 |
| 14.5625 | 5.6740 | ± | 0.1446 | 6.0602 |
| 14.9091 | 5.6672 | ± | 0.1509 | 6.0638 |
| 15.2281 | 5.6655 | ± | 0.1488 | 6.0717 |
| 15.5322 | 5.6528 | ± | 0.1543 | 6.0683 |
| 15.8042 | 5.6590 | ± | 0.1604 | 6.0828 |
| 16.0628 | 5.6561 | ± | 0.1646 | 6.0879 |
| 16.2990 | 5.6615 | ± | 0.1724 | 6.1006 |
| 16.5294 | 5.6490 | ± | 0.1797 | 6.0952 |
| 16.7349 | 5.6533 | ± | 0.1879 | 6.1059 |
| 16.9321 | 5.6475 | ± | 0.1838 | 6.1063 |
| 17.1070 | 5.6575 | ± | 0.1830 | 6.1219 |
| 17.2785 | 5.6531 | ± | 0.1867 | 6.1228 |
| 17.4444 | 5.6385 | ± | 0.2097 | 6.1135 |
| 17.5858 | 5.6470 | ± | 0.2095 | 6.1265 |
| 17.7190 | 5.6543 | ± | 0.2147 | 6.1380 |
| 17.8540 | 5.6422 | ± | 0.2320 | 6.1303 |
| 17.9737 | 5.6424 | ± | 0.2130 | 6.1343 |
| 18.0852 | 5.6434 | ± | 0.2237 | 6.1389 |
| 18.1848 | 5.6518 | ± | 0.2377 | 6.1505 |
| 18.2825 | 5.6523 | ± | 0.2314 | 6.1541 |
| 18.3740 | 5.6515 | ± | 0.2590 | 6.1563 |

Online resource 6: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 0.008 ± 0.005 ºC |  |  |  |  |
| 18.4622 | 5.6469 | ± | 0.3052 | 6.1546 |
| 18.5410 | 5.6491 | ± | 0.3146 | 6.1593 |
| 18.6114 | 5.6566 | ± | 0.3012 | 6.1691 |
| 18.6849 | 5.6497 | ± | 0.3036 | 6.1646 |
| 18.7546 | 5.6415 | ± | 0.3217 | 6.1587 |
| 18.8105 | 5.6523 | ± | 0.3308 | 6.1713 |
| 18.8709 | 5.6458 | ± | 0.3298 | 6.1668 |
| 18.9251 | 5.6452 | ± | 0.3702 | 6.1680 |
| 18.9670 | 5.6601 | ± | 0.3596 | 6.1843 |
| 19.0223 | 5.6446 | ± | 0.3117 | 6.1706 |
| T = 25.009 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.1819 | 3.5531 | ± | 0.0051 | 3.5570 |
| 0.3016 | 3.7492 | ± | 0.0087 | 3.7558 |
| 0.4437 | 3.9017 | ± | 0.0125 | 3.9114 |
| 0.5944 | 4.0273 | ± | 0.0136 | 4.0403 |
| 0.7542 | 4.1254 | ± | 0.0156 | 4.1418 |
| 0.9175 | 4.2032 | ± | 0.0175 | 4.2232 |
| 1.0784 | 4.2681 | ± | 0.0165 | 4.2917 |
| 1.2323 | 4.3265 | ± | 0.0194 | 4.3534 |
| 1.3904 | 4.3654 | ± | 0.0173 | 4.3958 |
| 1.5274 | 4.4163 | ± | 0.0190 | 4.4497 |
| 1.6705 | 4.4468 | ± | 0.0214 | 4.4835 |
| 1.8045 | 4.4761 | ± | 0.0217 | 4.5157 |
| 1.9277 | 4.5070 | ± | 0.0244 | 4.5493 |
| 2.0492 | 4.5289 | ± | 0.0257 | 4.5740 |
| 2.1568 | 4.5577 | ± | 0.0296 | 4.6051 |
| 2.2594 | 4.5832 | ± | 0.0330 | 4.6329 |
| 2.3608 | 4.6009 | ± | 0.0340 | 4.6529 |
| 2.4624 | 4.6096 | ± | 0.0323 | 4.6638 |
| 2.5424 | 4.6368 | ± | 0.0298 | 4.6928 |
| 2.6375 | 4.6381 | ± | 0.0316 | 4.6962 |
| 2.7159 | 4.6522 | ± | 0.0359 | 4.7121 |
| 2.7893 | 4.6661 | ± | 0.0411 | 4.7276 |
| 2.8562 | 4.6815 | ± | 0.0476 | 4.7445 |

Online resource 6: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 25.009 ± 0.005 K |  |  |  |  |
| 2.9280 | 4.6851 | ± | 0.0487 | 4.7497 |
| 2.9859 | 4.7001 | ± | 0.0496 | 4.7660 |
| 3.0462 | 4.7071 | ± | 0.0560 | 4.7743 |
| 3.0986 | 4.7187 | ± | 0.0574 | 4.7872 |
| 3.1572 | 4.7182 | ± | 0.0551 | 4.7880 |
| 3.2063 | 4.7248 | ± | 0.0586 | 4.7957 |
| 3.2476 | 4.7371 | ± | 0.0553 | 4.8089 |
| 3.2901 | 4.7462 | ± | 0.0507 | 4.8189 |
| 3.7444 | 4.7872 | ± | 0.0450 | 4.8702 |
| 4.1701 | 4.8238 | ± | 0.0347 | 4.9164 |
| 4.5704 | 4.8550 | ± | 0.0386 | 4.9567 |
| 4.9467 | 4.8816 | ± | 0.0410 | 4.9919 |
| 5.3203 | 4.8784 | ± | 0.0440 | 4.9973 |
| 5.6522 | 4.8969 | ± | 0.0454 | 5.0234 |
| 5.9633 | 4.9129 | ± | 0.0481 | 5.0466 |
| 6.2597 | 4.9206 | ± | 0.0519 | 5.0612 |
| 6.5290 | 4.9375 | ± | 0.0532 | 5.0844 |
| 6.7882 | 4.9442 | ± | 0.0541 | 5.0971 |
| 7.0255 | 4.9568 | ± | 0.0581 | 5.1152 |
| 7.2595 | 4.9529 | ± | 0.0605 | 5.1168 |
| 7.4651 | 4.9661 | ± | 0.0656 | 5.1349 |
| 7.6653 | 4.9684 | ± | 0.0667 | 5.1419 |
| 7.8456 | 4.9794 | ± | 0.0690 | 5.1571 |
| 8.0186 | 4.9845 | ± | 0.0718 | 5.1663 |
| 8.1800 | 4.9896 | ± | 0.0725 | 5.1752 |
| 8.3309 | 4.9948 | ± | 0.0756 | 5.1840 |
| 8.4718 | 4.9999 | ± | 0.0785 | 5.1924 |
| 8.6033 | 5.0051 | ± | 0.0770 | 5.2008 |
| 8.7352 | 4.9984 | ± | 0.0783 | 5.1972 |
| 8.8429 | 5.0129 | ± | 0.0791 | 5.2143 |
| 8.9551 | 5.0114 | ± | 0.0883 | 5.2155 |
| 9.0605 | 5.0094 | ± | 0.0970 | 5.2160 |
| 9.1531 | 5.0153 | ± | 0.1051 | 5.2241 |
| 9.2476 | 5.0110 | ± | 0.1063 | 5.2221 |
| 9.3249 | 5.0215 | ± | 0.1048 | 5.2344 |
| 9.4092 | 5.0153 | ± | 0.1064 | 5.2303 |

Online resource 6: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 25.009 ± 0.005 ºC |  |  |  |  |
| 9.4819 | 5.0178 | ± | 0.1074 | 5.2345 |
| 9.5446 | 5.0276 | ± | 0.1093 | 5.2458 |
| 9.6095 | 5.0287 | ± | 0.1178 | 5.2485 |
| 9.6749 | 5.0235 | ± | 0.1143 | 5.2449 |
| 9.7282 | 5.0292 | ± | 0.1225 | 5.2518 |
| 9.7758 | 5.0379 | ± | 0.1424 | 5.2617 |
| 9.8282 | 5.0358 | ± | 0.1485 | 5.2609 |
| 9.8780 | 5.0326 | ± | 0.1549 | 5.2589 |
| 9.9189 | 5.0371 | ± | 0.1660 | 5.2644 |
| 10.0038 | 5.0310 | ± | 0.1539 | 5.2603 |
| 11.4140 | 5.0526 | ± | 0.2379 | 5.3164 |
| 12.5098 | 5.0591 | ± | 0.0986 | 5.3500 |
| 13.5327 | 5.0514 | ± | 0.1076 | 5.3680 |
| 14.4776 | 5.0460 | ± | 0.1157 | 5.3867 |
| 15.3572 | 5.0337 | ± | 0.1229 | 5.3970 |
| 16.1648 | 5.0331 | ± | 0.1299 | 5.4173 |
| 16.9125 | 5.0332 | ± | 0.1365 | 5.4371 |
| 17.6192 | 5.0141 | ± | 0.1431 | 5.4368 |
| 18.2719 | 5.0008 | ± | 0.1493 | 5.4409 |
| 18.8704 | 4.9994 | ± | 0.1554 | 5.4557 |
| 19.4326 | 4.9883 | ± | 0.1609 | 5.4598 |
| 19.9497 | 4.9859 | ± | 0.1654 | 5.4716 |
| 20.4378 | 4.9730 | ± | 0.1700 | 5.4722 |
| 20.8904 | 4.9629 | ± | 0.1749 | 5.4747 |
| 21.3002 | 4.9712 | ± | 0.1790 | 5.4945 |
| 21.6887 | 4.9680 | ± | 0.1829 | 5.5022 |
| 22.0557 | 4.9574 | ± | 0.1868 | 5.5020 |
| 22.3950 | 4.9510 | ± | 0.1911 | 5.5052 |
| 22.7089 | 4.9488 | ± | 0.1937 | 5.5120 |
| 23.0036 | 4.9433 | ± | 0.1985 | 5.5150 |
| 23.2858 | 4.9261 | ± | 0.2022 | 5.5060 |
| 24.0010 | 4.9163 | ± | 0.2114 | 5.5170 |
| 24.2011 | 4.9251 | ± | 0.2181 | 5.5316 |
| 24.3903 | 4.9306 | ± | 0.2202 | 5.5427 |
| 24.5801 | 4.9134 | ± | 0.2267 | 5.5311 |
| 24.7466 | 4.9150 | ± | 0.2324 | 5.5376 |

Online resource 6: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 25.009 ± 0.005 ºC |  |  |  |  |
| 24.9077 | 4.9079 | ± | 0.2317 | 5.5353 |
| 25.0542 | 4.9062 | ± | 0.2431 | 5.5379 |
| 25.1906 | 4.9069 | ± | 0.2507 | 5.5427 |
| 25.3197 | 4.9048 | ± | 0.2506 | 5.5444 |
| 25.4365 | 4.9092 | ± | 0.2526 | 5.5523 |
| 25.5554 | 4.8973 | ± | 0.2513 | 5.5439 |
| 25.6562 | 4.9024 | ± | 0.2772 | 5.5521 |
| 25.7557 | 4.8997 | ± | 0.2937 | 5.5524 |
| 25.8488 | 4.8970 | ± | 0.2963 | 5.5525 |
| 25.9363 | 4.8929 | ± | 0.3021 | 5.5510 |
| 26.0110 | 4.9019 | ± | 0.3085 | 5.5623 |
| 26.0886 | 4.8975 | ± | 0.3588 | 5.5602 |
| 26.1574 | 4.8995 | ± | 0.3822 | 5.5643 |
| 26.2214 | 4.9022 | ± | 0.3838 | 5.5690 |
| 26.2824 | 4.9034 | ± | 0.3891 | 5.5720 |
| 26.3400 | 4.9027 | ± | 0.3589 | 5.5731 |
| 26.3987 | 4.8953 | ± | 0.3636 | 5.5674 |
| 26.4419 | 4.9069 | ± | 0.4116 | 5.5804 |
| 26.4928 | 4.9002 | ± | 0.4291 | 5.5752 |
| 26.5355 | 4.9029 | ± | 0.4817 | 5.5792 |
| 26.5764 | 4.9041 | ± | 0.4937 | 5.5816 |
| 26.6114 | 4.9110 | ± | 0.5213 | 5.5896 |
| 26.6537 | 4.9027 | ± | 0.5312 | 5.5826 |
| 27.7826 | 4.8620 | ± | 0.3807 | 5.5767 |
| 28.8080 | 4.8450 | ± | 0.2520 | 5.5918 |
| 29.7688 | 4.7985 | ± | 0.2619 | 5.5760 |
| 30.6386 | 4.7796 | ± | 0.2710 | 5.5853 |
| 31.4454 | 4.7539 | ± | 0.2806 | 5.5862 |
| 32.1947 | 4.7199 | ± | 0.2899 | 5.5773 |
| 32.8807 | 4.6986 | ± | 0.2990 | 5.5793 |
| 33.5214 | 4.6663 | ± | 0.3055 | 5.5691 |
| 34.1035 | 4.6550 | ± | 0.3128 | 5.5780 |
| 34.6451 | 4.6380 | ± | 0.3196 | 5.5801 |
| 35.1496 | 4.6171 | ± | 0.3258 | 5.5771 |
| 35.6128 | 4.6058 | ± | 0.3316 | 5.5824 |
| 36.0464 | 4.5860 | ± | 0.3366 | 5.5784 |

Online resource 6: continued.

| p | nexc (Helium) |  |  |  |  |  | na |
| --- | --- | --- | --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  |  |  |  | /(mmol∙g-1) |
| T = 298.159 ± 0.005 K |  |  |  |  |  |  |  |
| 36.4522 | 4.5629 |  | ± |  | 0.3418 |  | 5.5702 |
| 36.8197 | 4.5565 |  | ± |  | 0.3507 |  | 5.5773 |
| 37.1642 | 4.5461 |  | ± |  | 0.3596 |  | 5.5797 |
| 37.4841 | 4.5366 |  | ± |  | 0.3666 |  | 5.5823 |
| 37.7834 | 4.5218 |  | ± |  | 0.3701 |  | 5.5788 |
| 38.0629 | 4.5074 |  | ± |  | 0.3737 |  | 5.5750 |
| 38.3234 | 4.4926 |  | ± |  | 0.3765 |  | 5.5702 |
| 38.5567 | 4.4978 |  | ± |  | 0.3839 |  | 5.5844 |
| 38.7808 | 4.4876 |  | ± |  | 0.3908 |  | 5.5828 |
| 38.9924 | 4.4728 |  | ± |  | 0.3896 |  | 5.5763 |
| 39.1777 | 4.4841 |  | ± |  | 0.3926 |  | 5.5949 |
| 39.3623 | 4.4665 |  | ± |  | 0.4169 |  | 5.5846 |
| 39.5302 | 4.4632 |  | ± |  | 0.4309 |  | 5.5878 |
| 39.6885 | 4.4509 |  | ± |  | 0.4270 |  | 5.5819 |
| 39.8304 | 4.4535 |  | ± |  | 0.4446 |  | 5.5900 |
| 39.9574 | 4.4648 |  | ± |  | 0.4474 |  | 5.6065 |
| 40.0869 | 4.4548 |  | ± |  | 0.4496 |  | 5.6016 |
| T = 323.161 ± 0.005 K |  |  |  |  |  |  |  |
| 0.0000 | 0.0000 |  | ± | 0.0000 |  |  | 0.0000 |
| 0.2141 | 3.1481 |  | ± | 0.0051 |  |  | 3.1524 |
| 1.0682 | 3.7926 |  | ± | 0.0098 |  |  | 3.8141 |
| 2.1916 | 4.0457 |  | ± | 0.0165 |  |  | 4.0901 |
| 3.3186 | 4.1970 |  | ± | 0.0244 |  |  | 4.2645 |
| 4.4188 | 4.2853 |  | ± | 0.0317 |  |  | 4.3755 |
| 5.4671 | 4.3444 |  | ± | 0.0388 |  |  | 4.4564 |
| 6.4542 | 4.3903 |  | ± | 0.0458 |  |  | 4.5231 |
| 7.3863 | 4.4216 |  | ± | 0.0525 |  |  | 4.5741 |
| 8.2625 | 4.4442 |  | ± | 0.0590 |  |  | 4.6155 |
| 9.0862 | 4.4595 |  | ± | 0.0648 |  |  | 4.6485 |
| 9.8573 | 4.4725 |  | ± | 0.0705 |  |  | 4.6782 |
| 10.5759 | 4.4867 |  | ± | 0.0755 |  |  | 4.7080 |
| 11.2526 | 4.4942 |  | ± | 0.0804 |  |  | 4.7304 |
| 11.8918 | 4.4928 |  | ± | 0.0856 |  |  | 4.7430 |
| 12.4813 | 4.5011 |  | ± | 0.0900 |  |  | 4.7644 |
| 13.0427 | 4.4974 |  | ± | 0.0946 |  |  | 4.7731 |

Online resource 6: continued.

| p | nexc (Helium) |  |  |  | na |
| --- | --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  |  | /(mmol∙g-1) |
| T = 323.161 ± 0.005 K |  |  |  |  |  |
| 13.5651 | 4.4964 | ± | 0.0994 | 4.7838 |  |
| 14.0501 | 4.4994 | ± | 0.1026 | 4.7977 |  |
| 14.5115 | 4.4916 | ± | 0.1068 | 4.8003 |  |
| 14.9335 | 4.4958 | ± | 0.1106 | 4.8141 |  |
| 15.3319 | 4.4949 | ± | 0.1129 | 4.8222 |  |
| 15.7133 | 4.4821 | ± | 0.1171 | 4.8181 |  |
| 16.0637 | 4.4778 | ± | 0.1205 | 4.8219 |  |
| 16.3828 | 4.4837 | ± | 0.1211 | 4.8351 |  |
| 16.6911 | 4.4769 | ± | 0.1252 | 4.8354 |  |
| 16.9849 | 4.4625 | ± | 0.1292 | 4.8278 |  |
| 17.2378 | 4.4768 | ± | 0.1302 | 4.8480 |  |
| 17.4889 | 4.4712 | ± | 0.1348 | 4.8482 |  |
| 17.7218 | 4.4685 | ± | 0.1418 | 4.8509 |  |
| 17.9353 | 4.4711 | ± | 0.1471 | 4.8585 |  |
| 20.5753 | 4.4120 | ± | 0.1620 | 4.8617 |  |
| 22.1780 | 4.3756 | ± | 0.1647 | 4.8640 |  |
| 23.6482 | 4.3548 | ± | 0.1767 | 4.8792 |  |
| 25.0164 | 4.3217 | ± | 0.1887 | 4.8800 |  |
| 26.2805 | 4.2915 | ± | 0.1993 | 4.8817 |  |
| 27.4503 | 4.2630 | ± | 0.2088 | 4.8829 |  |
| 28.5315 | 4.2383 | ± | 0.2185 | 4.8861 |  |
| 29.5399 | 4.2057 | ± | 0.2284 | 4.8799 |  |
| 30.4689 | 4.1823 | ± | 0.2372 | 4.8810 |  |
| 31.3396 | 4.1474 | ± | 0.2445 | 4.8692 |  |
| 32.1377 | 4.1301 | ± | 0.2525 | 4.8734 |  |
| 32.8828 | 4.1063 | ± | 0.2594 | 4.8698 |  |
| 33.5676 | 4.0964 | ± | 0.2653 | 4.8786 |  |
| 34.2130 | 4.0744 | ± | 0.2719 | 4.8744 |  |
| 34.8160 | 4.0484 | ± | 0.2781 | 4.8651 |  |
| 35.3695 | 4.0350 | ± | 0.2842 | 4.8672 |  |
| 35.8861 | 4.0201 | ± | 0.2917 | 4.8669 |  |
| 36.3663 | 4.0082 | ± | 0.2990 | 4.8686 |  |
| 36.8135 | 3.9949 | ± | 0.3006 | 4.8679 |  |
| 38.1274 | 3.9565 | ± | 0.3126 | 4.8673 |  |
| 38.9459 | 3.9284 | ± | 0.3185 | 4.8631 |  |
| 39.6994 | 3.9133 | ± | 0.3251 | 4.8702 |  |
| 40.4089 | 3.8807 | ± | 0.3321 | 4.8587 |  |

Online resource 7: Absolute and excess COS adsorption on zeolite 4A at 0.012, 24.994, 49.997 ºC

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 0.012 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.0565 | 0.3330 | ± | 0.0007 | 0.3342 |
| 0.0758 | 0.4426 | ± | 0.0009 | 0.4442 |
| 0.0819 | 0.5523 | ± | 0.0011 | 0.5540 |
| 0.0864 | 0.6560 | ± | 0.0013 | 0.6578 |
| 0.0918 | 0.7526 | ± | 0.0015 | 0.7546 |
| 0.0997 | 0.8416 | ± | 0.0017 | 0.8437 |
| 0.1079 | 0.9247 | ± | 0.0019 | 0.9270 |
| 0.1252 | 0.9968 | ± | 0.0021 | 0.9994 |
| 0.1358 | 1.0676 | ± | 0.0022 | 1.0704 |
| 0.1506 | 1.1310 | ± | 0.0024 | 1.1341 |
| 0.1576 | 1.1945 | ± | 0.0025 | 1.1978 |
| 0.1595 | 1.2567 | ± | 0.0027 | 1.2601 |
| 0.1641 | 1.3136 | ± | 0.0028 | 1.3171 |
| 0.1724 | 1.3646 | ± | 0.0029 | 1.3682 |
| 0.1831 | 1.4106 | ± | 0.0030 | 1.4145 |
| 0.1994 | 1.4528 | ± | 0.0031 | 1.4570 |
| 0.2493 | 1.5492 | ± | 0.0033 | 1.5544 |
| 0.2827 | 1.6464 | ± | 0.0036 | 1.6524 |
| 0.3110 | 1.7387 | ± | 0.0038 | 1.7453 |
| 0.3333 | 1.8273 | ± | 0.0041 | 1.8343 |
| 0.3565 | 1.9083 | ± | 0.0043 | 1.9159 |
| 0.3804 | 1.9826 | ± | 0.0045 | 1.9906 |
| 0.4074 | 2.0489 | ± | 0.0046 | 2.0575 |
| 0.4468 | 2.1019 | ± | 0.0048 | 2.1113 |
| 0.4816 | 2.1519 | ± | 0.0050 | 2.1621 |
| 0.5124 | 2.1992 | ± | 0.0052 | 2.2101 |
| 0.5393 | 2.2441 | ± | 0.0054 | 2.2556 |
| 0.5549 | 2.2915 | ± | 0.0055 | 2.3032 |
| 0.5622 | 2.3400 | ± | 0.0057 | 2.3519 |
| 0.5714 | 2.3839 | ± | 0.0058 | 2.3960 |
| 0.5902 | 2.4186 | ± | 0.0059 | 2.4311 |
| 0.6223 | 2.4418 | ± | 0.0060 | 2.4550 |
| 0.6441 | 2.4680 | ± | 0.0061 | 2.4817 |
| 0.6615 | 2.4938 | ± | 0.0063 | 2.5079 |
| 0.6677 | 2.5179 | ± | 0.0065 | 2.5321 |

Online resource 7: continued

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 0.012 ± 0.005 ºC |  |  |  |  |
| 0.6710 | 2.5454 | ± | 0.0067 | 2.5597 |
| 0.6718 | 2.5785 | ± | 0.0066 | 2.5928 |
| 0.6728 | 2.6093 | ± | 0.0066 | 2.6236 |
| 0.6748 | 2.6340 | ± | 0.0068 | 2.6483 |
| 0.6979 | 2.6455 | ± | 0.0070 | 2.6603 |
| 0.8199 | 2.6951 | ± | 0.0070 | 2.7125 |
| 0.9078 | 2.7544 | ± | 0.0072 | 2.7738 |
| 0.9784 | 2.8148 | ± | 0.0075 | 2.8357 |
| 1.0474 | 2.8675 | ± | 0.0078 | 2.8899 |
| 1.1172 | 2.9118 | ± | 0.0081 | 2.9356 |
| 1.2015 | 2.9394 | ± | 0.0085 | 2.9652 |
| 1.2887 | 2.9579 | ± | 0.0088 | 2.9855 |
| 1.3646 | 2.9761 | ± | 0.0091 | 3.0054 |
| 1.4303 | 2.9944 | ± | 0.0093 | 3.0251 |
| 1.4811 | 3.0162 | ± | 0.0096 | 3.0480 |
| 1.5224 | 3.0388 | ± | 0.0099 | 3.0715 |
| 1.5663 | 3.0552 | ± | 0.0101 | 3.0890 |
| 1.6132 | 3.0655 | ± | 0.0102 | 3.1002 |
| 1.6631 | 3.0722 | ± | 0.0104 | 3.1080 |
| T = 24.994 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.0598 | 0.5069 | ± | 0.0008 | 0.5080 |
| 0.0870 | 0.7375 | ± | 0.0012 | 0.7392 |
| 0.1191 | 0.9505 | ± | 0.0015 | 0.9528 |
| 0.1528 | 1.1485 | ± | 0.0018 | 1.1514 |
| 0.1851 | 1.3338 | ± | 0.0022 | 1.3374 |
| 0.2197 | 1.5052 | ± | 0.0025 | 1.5094 |
| 0.2571 | 1.6630 | ± | 0.0027 | 1.6680 |
| 0.2945 | 1.8096 | ± | 0.0030 | 1.8153 |
| 0.3368 | 1.9428 | ± | 0.0033 | 1.9493 |
| 0.3773 | 2.0762 | ± | 0.0035 | 2.0835 |
| 0.5125 | 2.2636 | ± | 0.0041 | 2.2735 |
| 0.6452 | 2.4307 | ± | 0.0046 | 2.4433 |
| 0.7814 | 2.5757 | ± | 0.0051 | 2.5908 |
| 0.9299 | 2.6946 | ± | 0.0056 | 2.7127 |

Online resource 7: continued

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 24.994 ± 0.005 ºC |  |  |  |  |
| 1.0877 | 2.7900 | ± | 0.0061 | 2.8112 |
| 1.2558 | 2.8623 | ± | 0.0067 | 2.8868 |
| 1.4283 | 2.9157 | ± | 0.0073 | 2.9436 |
| 1.6028 | 2.9526 | ± | 0.0079 | 2.9840 |
| 1.7789 | 2.9742 | ± | 0.0085 | 3.0092 |
| 1.9549 | 2.9890 | ± | 0.0090 | 3.0275 |
| 2.4210 | 3.0132 | ± | 0.0106 | 3.0611 |
| 2.8470 | 3.0277 | ± | 0.0121 | 3.0844 |
| 3.2371 | 3.0335 | ± | 0.0135 | 3.0982 |
| 3.5906 | 3.0338 | ± | 0.0148 | 3.1059 |
| T = 49.997 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.0513 | 0.2428 | ± | 0.0004 | 0.2437 |
| 0.1021 | 0.4700 | ± | 0.0008 | 0.4718 |
| 0.1545 | 0.6813 | ± | 0.0012 | 0.6841 |
| 0.2143 | 0.8747 | ± | 0.0016 | 0.8785 |
| 0.2741 | 1.0544 | ± | 0.0019 | 1.0593 |
| 0.3295 | 1.2233 | ± | 0.0023 | 1.2292 |
| 0.3859 | 1.3794 | ± | 0.0026 | 1.3862 |
| 0.4472 | 1.5214 | ± | 0.0029 | 1.5294 |
| 0.5085 | 1.6523 | ± | 0.0032 | 1.6614 |
| 0.5706 | 1.7724 | ± | 0.0035 | 1.7826 |
| 0.6321 | 1.8828 | ± | 0.0037 | 1.8941 |
| 0.6932 | 1.9840 | ± | 0.0040 | 1.9964 |
| 0.7539 | 2.0766 | ± | 0.0043 | 2.0901 |
| 0.8147 | 2.1607 | ± | 0.0045 | 2.1753 |
| 0.8767 | 2.2362 | ± | 0.0048 | 2.2519 |
| 0.9397 | 2.3037 | ± | 0.0050 | 2.3205 |
| 1.0007 | 2.3651 | ± | 0.0052 | 2.3830 |
| 1.0612 | 2.4200 | ± | 0.0055 | 2.4390 |
| 1.1217 | 2.4684 | ± | 0.0057 | 2.4886 |
| 1.1845 | 2.5098 | ± | 0.0060 | 2.5311 |
| 1.2508 | 2.5436 | ± | 0.0062 | 2.5660 |
| 1.3123 | 2.5744 | ± | 0.0064 | 2.5980 |
| 1.5944 | 2.7122 | ± | 0.0072 | 2.7410 |

Online resource 7: continued

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 49.997 ± 0.005 ºC |  |  |  |  |
| 1.8966 | 2.7578 | ± | 0.0081 | 2.7921 |
| 2.1829 | 2.7920 | ± | 0.0090 | 2.8315 |
| 2.4522 | 2.8168 | ± | 0.0099 | 2.8613 |
| 2.7047 | 2.8336 | ± | 0.0107 | 2.8828 |
| 2.9379 | 2.8451 | ± | 0.0115 | 2.8987 |
| 3.1536 | 2.8516 | ± | 0.0122 | 2.9093 |
| 3.3510 | 2.8551 | ± | 0.0128 | 2.9164 |
| 3.5304 | 2.8564 | ± | 0.0135 | 2.9211 |
| 3.6945 | 2.8551 | ± | 0.0140 | 2.9230 |
| 3.8428 | 2.8526 | ± | 0.0146 | 2.9233 |
| 3.9746 | 2.8502 | ± | 0.0151 | 2.9234 |
| 4.0933 | 2.8469 | ± | 0.0155 | 2.9224 |

Online resource 8: Absolute and excess H2S adsorption on zeolite 4A at 0.004, 25.007, 49.976 ºC

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 0.004 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.0533 | 3.9896 | ± | 0.0077 | 3.9907 |
| 0.0585 | 4.1228 | ± | 0.0080 | 4.1241 |
| 0.0682 | 4.2450 | ± | 0.0083 | 4.2465 |
| 0.0828 | 4.3564 | ± | 0.0085 | 4.3581 |
| 0.1034 | 4.4566 | ± | 0.0087 | 4.4587 |
| 0.1309 | 4.5452 | ± | 0.0090 | 4.5480 |
| 0.1652 | 4.6227 | ± | 0.0092 | 4.6262 |
| 0.2059 | 4.6895 | ± | 0.0094 | 4.6938 |
| 0.2529 | 4.7457 | ± | 0.0095 | 4.7511 |
| 0.3042 | 4.7930 | ± | 0.0097 | 4.7994 |
| 0.3591 | 4.8319 | ± | 0.0099 | 4.8394 |
| 0.4156 | 4.8639 | ± | 0.0100 | 4.8727 |
| 0.4993 | 4.9328 | ± | 0.0102 | 4.9433 |
| 0.7688 | 5.0028 | ± | 0.0108 | 5.0191 |
| 1.0281 | 5.0564 | ± | 0.0115 | 5.0782 |
| 1.2773 | 5.0950 | ± | 0.0122 | 5.1222 |
| 1.5127 | 5.1224 | ± | 0.0129 | 5.1547 |
| 1.7303 | 5.1427 | ± | 0.0136 | 5.1798 |
| 1.9316 | 5.1566 | ± | 0.0142 | 5.1980 |
| 2.1175 | 5.1650 | ± | 0.0148 | 5.2105 |
| 2.2840 | 5.1718 | ± | 0.0154 | 5.2210 |
| 2.4363 | 5.1752 | ± | 0.0159 | 5.2278 |
| 2.5756 | 5.1756 | ± | 0.0164 | 5.2312 |
| 2.7006 | 5.1748 | ± | 0.0168 | 5.2332 |
| 2.8129 | 5.1730 | ± | 0.0172 | 5.2339 |
| 2.9149 | 5.1693 | ± | 0.0176 | 5.2325 |
| 3.0069 | 5.1647 | ± | 0.0181 | 5.2300 |
| T = 25.007 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.1064 | 3.4350 | ± | 0.0064 | 3.4371 |
| 0.1560 | 3.9067 | ± | 0.0074 | 3.9097 |
| 0.2663 | 4.3138 | ± | 0.0083 | 4.3189 |
| 0.5122 | 4.6141 | ± | 0.0092 | 4.6240 |
| 0.9090 | 4.7964 | ± | 0.0102 | 4.8140 |

Online resource 8: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 25.007 ± 0.005 ºC |  |  |  |  |
| 1.3823 | 4.8997 | ± | 0.0113 | 4.9266 |
| 1.8682 | 4.9598 | ± | 0.0124 | 4.9963 |
| 2.3310 | 4.9986 | ± | 0.0135 | 5.0443 |
| 2.7679 | 5.0205 | ± | 0.0146 | 5.0750 |
| 3.1727 | 5.0468 | ± | 0.0157 | 5.1094 |
| 3.8386 | 5.0531 | ± | 0.0174 | 5.1293 |
| 4.4303 | 5.0576 | ± | 0.0191 | 5.1460 |
| 4.9650 | 5.0553 | ± | 0.0206 | 5.1548 |
| 5.4438 | 5.0495 | ± | 0.0220 | 5.1591 |
| 5.8767 | 5.0386 | ± | 0.0233 | 5.1573 |
| 6.2670 | 5.0240 | ± | 0.0245 | 5.1510 |
| T = 49.976 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.0607 | 3.1484 | ± | 0.0061 | 3.1494 |
| 0.0796 | 3.2386 | ± | 0.0061 | 3.2400 |
| 0.0995 | 3.3226 | ± | 0.0064 | 3.3244 |
| 0.1214 | 3.4002 | ± | 0.0065 | 3.4024 |
| 0.1433 | 3.4727 | ± | 0.0067 | 3.4752 |
| 0.1648 | 3.5404 | ± | 0.0069 | 3.5434 |
| 0.1875 | 3.6030 | ± | 0.0071 | 3.6063 |
| 0.2127 | 3.6598 | ± | 0.0072 | 3.6636 |
| 0.2400 | 3.7149 | ± | 0.0074 | 3.7192 |
| 0.4681 | 4.0438 | ± | 0.0075 | 4.0521 |
| 0.8221 | 4.2779 | ± | 0.0081 | 4.2925 |
| 1.2691 | 4.4319 | ± | 0.0091 | 4.4547 |
| 1.7570 | 4.5318 | ± | 0.0103 | 4.5633 |
| 2.2456 | 4.5986 | ± | 0.0115 | 4.6391 |
| 2.7140 | 4.6450 | ± | 0.0128 | 4.6940 |
| 3.1558 | 4.6764 | ± | 0.0142 | 4.7336 |
| 3.5676 | 4.6971 | ± | 0.0155 | 4.7619 |
| 3.9461 | 4.7108 | ± | 0.0167 | 4.7827 |
| 4.2939 | 4.7187 | ± | 0.0178 | 4.7971 |
| 4.6147 | 4.7206 | ± | 0.0189 | 4.8050 |
| 4.9125 | 4.7163 | ± | 0.0199 | 4.8063 |
| 5.1797 | 4.7114 | ± | 0.0209 | 4.8064 |

Online resource 9: Absolute and excess CH4 adsorption on zeolite 4A at −0.160, 24.841, 49.839 ºC

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = −0.160 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.1525 | 0.2561 | ± | 0.0036 | 0.2620 |
| 0.3096 | 0.5081 | ± | 0.0079 | 0.5201 |
| 0.4777 | 0.7509 | ± | 0.0126 | 0.7693 |
| 0.6580 | 0.9834 | ± | 0.0174 | 1.0085 |
| 0.8525 | 1.2041 | ± | 0.0223 | 1.2362 |
| 1.0629 | 1.4117 | ± | 0.0273 | 1.4513 |
| 1.2915 | 1.6043 | ± | 0.0324 | 1.6518 |
| 1.5389 | 1.7813 | ± | 0.0376 | 1.8371 |
| 1.8057 | 1.9422 | ± | 0.0429 | 2.0068 |
| 2.0907 | 2.0877 | ± | 0.0483 | 2.1617 |
| 2.3933 | 2.2183 | ± | 0.0538 | 2.3021 |
| 2.7113 | 2.3356 | ± | 0.0593 | 2.4295 |
| 3.0433 | 2.4406 | ± | 0.0650 | 2.5451 |
| 3.3871 | 2.5349 | ± | 0.0708 | 2.6503 |
| 3.7416 | 2.6196 | ± | 0.0766 | 2.7461 |
| 4.1046 | 2.6963 | ± | 0.0825 | 2.8342 |
| 4.4753 | 2.7657 | ± | 0.0884 | 2.9151 |
| 4.8518 | 2.8292 | ± | 0.0944 | 2.9904 |
| 5.2343 | 2.8871 | ± | 0.1005 | 3.0601 |
| 5.6211 | 2.9405 | ± | 0.1066 | 3.1256 |
| 6.0111 | 2.9905 | ± | 0.1127 | 3.1877 |
| 6.4049 | 3.0362 | ± | 0.1189 | 3.2457 |
| 7.1619 | 3.0979 | ± | 0.0506 | 3.3267 |
| 7.9196 | 3.1578 | ± | 0.0728 | 3.4054 |
| 8.6885 | 3.2106 | ± | 0.0772 | 3.4774 |
| 9.4649 | 3.2579 | ± | 0.0815 | 3.5441 |
| 10.2447 | 3.3011 | ± | 0.0858 | 3.6069 |
| 11.0306 | 3.3390 | ± | 0.0901 | 3.6646 |
| 11.8188 | 3.3733 | ± | 0.0943 | 3.7188 |
| 12.6082 | 3.4043 | ± | 0.0986 | 3.7699 |
| 13.3980 | 3.4323 | ± | 0.1028 | 3.8180 |
| 14.1867 | 3.4580 | ± | 0.1070 | 3.8639 |
| 14.9745 | 3.4813 | ± | 0.1112 | 3.9074 |
| 15.7601 | 3.5027 | ± | 0.1154 | 3.9492 |
| 16.5428 | 3.5226 | ± | 0.1196 | 3.9894 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = −0.160 ± 0.005 ºC |  |  |  |  |
| 17.3232 | 3.5408 | ± | 0.1237 | 4.0278 |
| 18.1001 | 3.5576 | ± | 0.1279 | 4.0649 |
| 18.8740 | 3.5730 | ± | 0.1320 | 4.1006 |
| 19.6444 | 3.5872 | ± | 0.1361 | 4.1350 |
| 20.4111 | 3.6004 | ± | 0.1402 | 4.1684 |
| 21.1742 | 3.6124 | ± | 0.1442 | 4.2006 |
| 21.9358 | 3.6225 | ± | 0.1483 | 4.2310 |
| 22.6969 | 3.6303 | ± | 0.1523 | 4.2591 |
| 23.4483 | 3.6397 | ± | 0.1563 | 4.2887 |
| 24.1945 | 3.6489 | ± | 0.1603 | 4.3179 |
| 24.9369 | 3.6572 | ± | 0.1643 | 4.3463 |
| 25.6734 | 3.6656 | ± | 0.1683 | 4.3746 |
| 26.4172 | 3.6679 | ± | 0.1722 | 4.3972 |
| 27.1288 | 3.6815 | ± | 0.1762 | 4.4302 |
| 27.8471 | 3.6895 | ± | 0.1801 | 4.4579 |
| 28.5622 | 3.6963 | ± | 0.1840 | 4.4843 |
| 29.2739 | 3.7020 | ± | 0.1879 | 4.5096 |
| 29.9803 | 3.7075 | ± | 0.1917 | 4.5346 |
| 30.6822 | 3.7124 | ± | 0.1956 | 4.5590 |
| 31.3790 | 3.7171 | ± | 0.1994 | 4.5832 |
| 32.0716 | 3.7211 | ± | 0.2032 | 4.6066 |
| 32.7594 | 3.7248 | ± | 0.2070 | 4.6296 |
| 33.4419 | 3.7285 | ± | 0.2108 | 4.6525 |
| 34.1202 | 3.7316 | ± | 0.2145 | 4.6748 |
| 34.7941 | 3.7343 | ± | 0.2183 | 4.6966 |
| 35.4628 | 3.7370 | ± | 0.2220 | 4.7183 |
| 36.1272 | 3.7393 | ± | 0.2257 | 4.7395 |
| 36.7857 | 3.7418 | ± | 0.2294 | 4.7609 |
| 37.4401 | 3.7439 | ± | 0.2331 | 4.7817 |
| 38.0904 | 3.7455 | ± | 0.2367 | 4.8021 |
| 38.7361 | 3.7469 | ± | 0.2404 | 4.8222 |
| 39.3773 | 3.7481 | ± | 0.2440 | 4.8420 |
| 40.0136 | 3.7493 | ± | 0.2476 | 4.8617 |
| 40.6448 | 3.7506 | ± | 0.2512 | 4.8815 |
| 41.2732 | 3.7510 | ± | 0.2548 | 4.9002 |
| 41.8948 | 3.7523 | ± | 0.2583 | 4.9198 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = −0.160 ± 0.005 ºC |  |  |  |  |
| 42.5142 | 3.7524 | ± | 0.2619 | 4.9381 |
| 43.1288 | 3.7526 | ± | 0.2654 | 4.9564 |
| 43.7386 | 3.7528 | ± | 0.2689 | 4.9748 |
| 44.3441 | 3.7529 | ± | 0.2724 | 4.9929 |
| 44.9451 | 3.7530 | ± | 0.2759 | 5.0108 |
| 45.5424 | 3.7527 | ± | 0.2794 | 5.0284 |
| 46.1353 | 3.7524 | ± | 0.2828 | 5.0459 |
| 46.7248 | 3.7517 | ± | 0.2862 | 5.0629 |
| 47.3089 | 3.7515 | ± | 0.2897 | 5.0803 |
| 47.8894 | 3.7509 | ± | 0.2931 | 5.0973 |
| 48.4662 | 3.7500 | ± | 0.2965 | 5.1139 |
| 49.0383 | 3.7495 | ± | 0.2998 | 5.1308 |
| 49.6077 | 3.7482 | ± | 0.3032 | 5.1469 |
| 50.1731 | 3.7469 | ± | 0.3065 | 5.1629 |
| 50.7335 | 3.7460 | ± | 0.3099 | 5.1792 |
| 51.2914 | 3.7445 | ± | 0.3132 | 5.1948 |
| 51.8453 | 3.7429 | ± | 0.3165 | 5.2103 |
| 52.3953 | 3.7414 | ± | 0.3198 | 5.2257 |
| 52.9408 | 3.7402 | ± | 0.3230 | 5.2414 |
| 53.4825 | 3.7389 | ± | 0.3263 | 5.2570 |
| 54.0205 | 3.7376 | ± | 0.3295 | 5.2725 |
| 54.5547 | 3.7364 | ± | 0.3327 | 5.2879 |
| 55.0854 | 3.7350 | ± | 0.3360 | 5.3032 |
| 55.6130 | 3.7333 | ± | 0.3392 | 5.3180 |
| 56.1369 | 3.7315 | ± | 0.3423 | 5.3327 |
| 56.6568 | 3.7299 | ± | 0.3455 | 5.3475 |
| 57.1734 | 3.7281 | ± | 0.3487 | 5.3621 |
| 57.6868 | 3.7262 | ± | 0.3518 | 5.3764 |
| 58.1975 | 3.7238 | ± | 0.3549 | 5.3902 |
| 58.7037 | 3.7219 | ± | 0.3580 | 5.4044 |
| 59.2079 | 3.7193 | ± | 0.3611 | 5.4179 |
| 59.7076 | 3.7172 | ± | 0.3642 | 5.4318 |
| 60.2044 | 3.7149 | ± | 0.3673 | 5.4455 |
| 60.6960 | 3.7135 | ± | 0.3703 | 5.4599 |
| 61.1873 | 3.7106 | ± | 0.3734 | 5.4728 |
| 61.6746 | 3.7081 | ± | 0.3764 | 5.4860 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = −0.160 ± 0.005 ºC |  |  |  |  |
| 62.1579 | 3.7060 | ± | 0.3794 | 5.4995 |
| 62.6397 | 3.7029 | ± | 0.3824 | 5.5121 |
| 63.1172 | 3.7005 | ± | 0.3854 | 5.5252 |
| 63.5907 | 3.6986 | ± | 0.3884 | 5.5387 |
| 64.0622 | 3.6960 | ± | 0.3913 | 5.5515 |
| 64.5302 | 3.6937 | ± | 0.3943 | 5.5645 |
| T = 24.841 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.1971 | 0.1696 | ± | 0.0033 | 0.1741 |
| 0.4008 | 0.3340 | ± | 0.0071 | 0.3433 |
| 0.6110 | 0.4936 | ± | 0.0113 | 0.5076 |
| 0.8273 | 0.6471 | ± | 0.0155 | 0.6661 |
| 1.0510 | 0.7952 | ± | 0.0198 | 0.8194 |
| 1.2833 | 0.9369 | ± | 0.0242 | 0.9664 |
| 1.5246 | 1.0715 | ± | 0.0286 | 1.1066 |
| 1.7745 | 1.1993 | ± | 0.0330 | 1.2402 |
| 2.0333 | 1.3200 | ± | 0.0375 | 1.3669 |
| 2.3005 | 1.4339 | ± | 0.0421 | 1.4870 |
| 2.5763 | 1.5409 | ± | 0.0467 | 1.6004 |
| 2.8600 | 1.6415 | ± | 0.0513 | 1.7075 |
| 3.1514 | 1.7358 | ± | 0.0560 | 1.8086 |
| 3.4507 | 1.8237 | ± | 0.0607 | 1.9035 |
| 3.7564 | 1.9062 | ± | 0.0655 | 1.9931 |
| 4.0684 | 1.9833 | ± | 0.0703 | 2.0775 |
| 4.3862 | 2.0555 | ± | 0.0751 | 2.1570 |
| 4.7091 | 2.1231 | ± | 0.0800 | 2.2321 |
| 5.0369 | 2.1863 | ± | 0.0849 | 2.3030 |
| 5.3686 | 2.2458 | ± | 0.0898 | 2.3702 |
| 5.7044 | 2.3015 | ± | 0.0947 | 2.4339 |
| 6.0431 | 2.3540 | ± | 0.0997 | 2.4943 |
| 6.3849 | 2.4035 | ± | 0.1047 | 2.5518 |
| 6.7291 | 2.4506 | ± | 0.1097 | 2.6070 |
| 7.0756 | 2.4949 | ± | 0.1147 | 2.6594 |
| 7.7665 | 2.5434 | ± | 0.0787 | 2.7235 |
| 8.4238 | 2.6028 | ± | 0.0655 | 2.7976 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 24.841 ± 0.005 ºC |  |  |  |  |
| 9.0903 | 2.6573 | ± | 0.0690 | 2.8671 |
| 9.7663 | 2.7067 | ± | 0.0726 | 2.9318 |
| 10.4937 | 2.7354 | ± | 0.0761 | 2.9770 |
| 11.1941 | 2.7715 | ± | 0.0797 | 3.0290 |
| 11.8862 | 2.8083 | ± | 0.0832 | 3.0816 |
| 12.5790 | 2.8429 | ± | 0.0866 | 3.1319 |
| 13.2738 | 2.8747 | ± | 0.0901 | 3.1796 |
| 13.9700 | 2.9041 | ± | 0.0936 | 3.2250 |
| 14.6672 | 2.9312 | ± | 0.0970 | 3.2681 |
| 15.3649 | 2.9563 | ± | 0.1004 | 3.3093 |
| 16.0624 | 2.9796 | ± | 0.1038 | 3.3487 |
| 16.7594 | 3.0013 | ± | 0.1072 | 3.3865 |
| 17.4552 | 3.0215 | ± | 0.1106 | 3.4229 |
| 18.1494 | 3.0406 | ± | 0.1140 | 3.4581 |
| 18.8425 | 3.0582 | ± | 0.1173 | 3.4919 |
| 19.5368 | 3.0736 | ± | 0.1207 | 3.5235 |
| 20.2297 | 3.0879 | ± | 0.1240 | 3.5540 |
| 20.9197 | 3.1017 | ± | 0.1273 | 3.5840 |
| 21.6126 | 3.1129 | ± | 0.1306 | 3.6116 |
| 22.2788 | 3.1330 | ± | 0.1339 | 3.6473 |
| 22.9171 | 3.1624 | ± | 0.1372 | 3.6918 |
| 23.5906 | 3.1770 | ± | 0.1405 | 3.7224 |
| 24.2620 | 3.1900 | ± | 0.1437 | 3.7513 |
| 24.9338 | 3.2011 | ± | 0.1470 | 3.7784 |
| 25.5941 | 3.2149 | ± | 0.1502 | 3.8079 |
| 26.2569 | 3.2257 | ± | 0.1534 | 3.8346 |
| 26.9184 | 3.2350 | ± | 0.1566 | 3.8597 |
| 27.5775 | 3.2433 | ± | 0.1598 | 3.8839 |
| 28.2333 | 3.2510 | ± | 0.1630 | 3.9074 |
| 28.8854 | 3.2584 | ± | 0.1661 | 3.9305 |
| 29.5345 | 3.2653 | ± | 0.1693 | 3.9530 |
| 30.1796 | 3.2719 | ± | 0.1724 | 3.9753 |
| 30.8218 | 3.2780 | ± | 0.1755 | 3.9970 |
| 31.4605 | 3.2838 | ± | 0.1786 | 4.0183 |
| 32.0956 | 3.2893 | ± | 0.1817 | 4.0393 |
| 32.7272 | 3.2945 | ± | 0.1847 | 4.0600 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 24.841 ± 0.005 ºC |  |  |  |  |
| 33.3557 | 3.2993 | ± | 0.1878 | 4.0801 |
| 33.9801 | 3.3041 | ± | 0.1908 | 4.1002 |
| 34.6012 | 3.3085 | ± | 0.1939 | 4.1199 |
| 35.2201 | 3.3122 | ± | 0.1969 | 4.1389 |
| 35.8341 | 3.3163 | ± | 0.1999 | 4.1581 |
| 36.4451 | 3.3200 | ± | 0.2029 | 4.1769 |
| 37.0529 | 3.3234 | ± | 0.2058 | 4.1953 |
| 37.6563 | 3.3269 | ± | 0.2088 | 4.2139 |
| 38.2559 | 3.3305 | ± | 0.2118 | 4.2324 |
| 38.8525 | 3.3336 | ± | 0.2147 | 4.2504 |
| 39.4457 | 3.3366 | ± | 0.2176 | 4.2681 |
| 40.0363 | 3.3390 | ± | 0.2205 | 4.2853 |
| 40.6230 | 3.3415 | ± | 0.2234 | 4.3025 |
| 41.2069 | 3.3436 | ± | 0.2263 | 4.3193 |
| 41.7870 | 3.3457 | ± | 0.2292 | 4.3360 |
| 42.3636 | 3.3478 | ± | 0.2320 | 4.3526 |
| 42.9365 | 3.3499 | ± | 0.2349 | 4.3692 |
| 43.5069 | 3.3515 | ± | 0.2377 | 4.3852 |
| 44.0740 | 3.3530 | ± | 0.2405 | 4.4011 |
| 44.6373 | 3.3546 | ± | 0.2433 | 4.4170 |
| 45.1969 | 3.3563 | ± | 0.2461 | 4.4329 |
| 45.7543 | 3.3574 | ± | 0.2489 | 4.4482 |
| 46.3087 | 3.3583 | ± | 0.2517 | 4.4633 |
| 46.8595 | 3.3594 | ± | 0.2544 | 4.4784 |
| 47.4069 | 3.3604 | ± | 0.2572 | 4.4935 |
| 47.9504 | 3.3616 | ± | 0.2599 | 4.5086 |
| 48.4915 | 3.3624 | ± | 0.2626 | 4.5234 |
| 49.0293 | 3.3633 | ± | 0.2653 | 4.5381 |
| 49.5639 | 3.3641 | ± | 0.2680 | 4.5526 |
| 50.0957 | 3.3647 | ± | 0.2707 | 4.5670 |
| 50.6243 | 3.3653 | ± | 0.2734 | 4.5812 |
| 51.1486 | 3.3663 | ± | 0.2760 | 4.5958 |
| 51.6708 | 3.3668 | ± | 0.2787 | 4.6099 |
| 52.1899 | 3.3672 | ± | 0.2813 | 4.6238 |
| 52.7050 | 3.3680 | ± | 0.2840 | 4.6380 |
| 53.2186 | 3.3681 | ± | 0.2866 | 4.6515 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 24.841 ± 0.005 ºC |  |  |  |  |
| 53.7299 | 3.3679 | ± | 0.2892 | 4.6646 |
| 54.2380 | 3.3677 | ± | 0.2918 | 4.6777 |
| 54.7426 | 3.3678 | ± | 0.2943 | 4.6910 |
| 55.2453 | 3.3674 | ± | 0.2969 | 4.7038 |
| 55.7451 | 3.3669 | ± | 0.2994 | 4.7164 |
| 56.2413 | 3.3668 | ± | 0.3020 | 4.7294 |
| 56.7353 | 3.3663 | ± | 0.3045 | 4.7419 |
| 57.2252 | 3.3665 | ± | 0.3070 | 4.7550 |
| 57.7138 | 3.3659 | ± | 0.3095 | 4.7673 |
| 58.1984 | 3.3659 | ± | 0.3120 | 4.7801 |
| 58.6815 | 3.3653 | ± | 0.3145 | 4.7923 |
| 59.1616 | 3.3647 | ± | 0.3170 | 4.8045 |
| 59.6391 | 3.3642 | ± | 0.3195 | 4.8166 |
| 60.1132 | 3.3638 | ± | 0.3219 | 4.8289 |
| 60.5855 | 3.3631 | ± | 0.3244 | 4.8407 |
| 61.0565 | 3.3617 | ± | 0.3268 | 4.8519 |
| 61.5275 | 3.3593 | ± | 0.3292 | 4.8620 |
| 61.9964 | 3.3567 | ± | 0.3316 | 4.8720 |
| 62.4595 | 3.3557 | ± | 0.3340 | 4.8834 |
| 62.9193 | 3.3551 | ± | 0.3364 | 4.8951 |
| 63.3773 | 3.3541 | ± | 0.3388 | 4.9064 |
| 63.8405 | 3.3499 | ± | 0.3412 | 4.9146 |
| 64.2878 | 3.3515 | ± | 0.3436 | 4.9282 |
| 64.7388 | 3.3504 | ± | 0.3459 | 4.9393 |
| 65.1894 | 3.3484 | ± | 0.3483 | 4.9495 |
| 65.6317 | 3.3491 | ± | 0.3506 | 4.9621 |
| 66.0693 | 3.3506 | ± | 0.3529 | 4.9754 |
| 66.5062 | 3.3511 | ± | 0.3552 | 4.9877 |
| 66.9430 | 3.3505 | ± | 0.3575 | 4.9989 |
| 67.3763 | 3.3501 | ± | 0.3598 | 5.0104 |
| 67.8083 | 3.3493 | ± | 0.3621 | 5.0212 |
| 68.2369 | 3.3488 | ± | 0.3644 | 5.0324 |
| 68.6638 | 3.3478 | ± | 0.3666 | 5.0431 |
| 69.0881 | 3.3470 | ± | 0.3689 | 5.0538 |
| 69.5099 | 3.3462 | ± | 0.3711 | 5.0645 |
| 69.9298 | 3.3452 | ± | 0.3733 | 5.0750 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 24.841 ± 0.005 ºC |  |  |  |  |
| 70.3476 | 3.3440 | ± | 0.3755 | 5.0852 |
| 70.7627 | 3.3430 | ± | 0.3777 | 5.0955 |
| 71.1796 | 3.3402 | ± | 0.3799 | 5.1042 |
| 71.5956 | 3.3370 | ± | 0.3821 | 5.1123 |
| T = 49.839 ± 0.005 ºC |  |  |  |  |
| 0.0000 | 0.0000 | ± | 0.0000 | 0.0000 |
| 0.2073 | 0.1007 | ± | 0.0028 | 0.1051 |
| 0.4170 | 0.1985 | ± | 0.0059 | 0.2073 |
| 0.6290 | 0.2937 | ± | 0.0093 | 0.3070 |
| 0.8430 | 0.3859 | ± | 0.0127 | 0.4038 |
| 1.0595 | 0.4753 | ± | 0.0161 | 0.4978 |
| 1.2789 | 0.5623 | ± | 0.0195 | 0.5894 |
| 1.5019 | 0.6463 | ± | 0.0230 | 0.6782 |
| 1.7278 | 0.7281 | ± | 0.0265 | 0.7648 |
| 1.9568 | 0.8074 | ± | 0.0299 | 0.8490 |
| 2.1891 | 0.8841 | ± | 0.0334 | 0.9307 |
| 2.4249 | 0.9582 | ± | 0.0370 | 1.0098 |
| 2.6634 | 1.0302 | ± | 0.0405 | 1.0868 |
| 2.9050 | 1.0997 | ± | 0.0441 | 1.1615 |
| 3.1505 | 1.1666 | ± | 0.0476 | 1.2337 |
| 3.3987 | 1.2318 | ± | 0.0512 | 1.3041 |
| 3.6508 | 1.2946 | ± | 0.0549 | 1.3724 |
| 4.0979 | 1.3788 | ± | 0.0390 | 1.4657 |
| 4.5339 | 1.4662 | ± | 0.0339 | 1.5620 |
| 4.9809 | 1.5492 | ± | 0.0367 | 1.6541 |
| 5.4331 | 1.6296 | ± | 0.0394 | 1.7438 |
| 5.8967 | 1.7050 | ± | 0.0422 | 1.8285 |
| 6.3725 | 1.7753 | ± | 0.0449 | 1.9086 |
| 6.8591 | 1.8410 | ± | 0.0476 | 1.9843 |
| 7.3547 | 1.9028 | ± | 0.0504 | 2.0563 |
| 7.8587 | 1.9610 | ± | 0.0531 | 2.1248 |
| 8.3720 | 2.0151 | ± | 0.0558 | 2.1895 |
| 8.8912 | 2.0663 | ± | 0.0584 | 2.2515 |
| 9.4166 | 2.1146 | ± | 0.0611 | 2.3106 |
| 9.9475 | 2.1600 | ± | 0.0638 | 2.3669 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 49.839 ± 0.005 ºC |  |  |  |  |
| 10.4885 | 2.2012 | ± | 0.0665 | 2.4194 |
| 11.0348 | 2.2401 | ± | 0.0691 | 2.4696 |
| 11.5809 | 2.2782 | ± | 0.0718 | 2.5190 |
| 12.1316 | 2.3138 | ± | 0.0744 | 2.5661 |
| 12.6873 | 2.3470 | ± | 0.0771 | 2.6108 |
| 13.2431 | 2.3792 | ± | 0.0797 | 2.6547 |
| 13.7964 | 2.4111 | ± | 0.0823 | 2.6981 |
| 14.3524 | 2.4405 | ± | 0.0849 | 2.7391 |
| 14.9103 | 2.4680 | ± | 0.0875 | 2.7783 |
| 15.4680 | 2.4944 | ± | 0.0901 | 2.8164 |
| 16.0296 | 2.5184 | ± | 0.0927 | 2.8522 |
| 16.5915 | 2.5413 | ± | 0.0953 | 2.8868 |
| 17.1532 | 2.5632 | ± | 0.0978 | 2.9206 |
| 17.7163 | 2.5835 | ± | 0.1004 | 2.9528 |
| 18.2750 | 2.6042 | ± | 0.1029 | 2.9853 |
| 18.8374 | 2.6226 | ± | 0.1055 | 3.0155 |
| 19.4016 | 2.6396 | ± | 0.1080 | 3.0445 |
| 19.9724 | 2.6535 | ± | 0.1105 | 3.0704 |
| 20.5311 | 2.6705 | ± | 0.1130 | 3.0993 |
| 21.0969 | 2.6840 | ± | 0.1155 | 3.1248 |
| 21.6573 | 2.6982 | ± | 0.1180 | 3.1509 |
| 22.2133 | 2.7148 | ± | 0.1205 | 3.1794 |
| 22.7685 | 2.7310 | ± | 0.1230 | 3.2074 |
| 23.3270 | 2.7449 | ± | 0.1255 | 3.2333 |
| 23.8892 | 2.7567 | ± | 0.1280 | 3.2571 |
| 24.4451 | 2.7697 | ± | 0.1304 | 3.2820 |
| 25.0034 | 2.7810 | ± | 0.1329 | 3.3052 |
| 25.5598 | 2.7919 | ± | 0.1353 | 3.3281 |
| 26.1151 | 2.8023 | ± | 0.1378 | 3.3504 |
| 26.6665 | 2.8129 | ± | 0.1402 | 3.3729 |
| 27.2132 | 2.8241 | ± | 0.1427 | 3.3959 |
| 27.7638 | 2.8329 | ± | 0.1451 | 3.4165 |
| 28.3092 | 2.8424 | ± | 0.1475 | 3.4378 |
| 28.8525 | 2.8515 | ± | 0.1499 | 3.4587 |
| 29.3961 | 2.8595 | ± | 0.1523 | 3.4785 |
| 29.9348 | 2.8681 | ± | 0.1546 | 3.4988 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 49.839 ± 0.005 ºC |  |  |  |  |
| 30.4720 | 2.8762 | ± | 0.1570 | 3.5185 |
| 31.0107 | 2.8826 | ± | 0.1594 | 3.5367 |
| 31.5443 | 2.8899 | ± | 0.1617 | 3.5556 |
| 32.0755 | 2.8971 | ± | 0.1641 | 3.5743 |
| 32.6067 | 2.9033 | ± | 0.1664 | 3.5921 |
| 33.1337 | 2.9100 | ± | 0.1687 | 3.6103 |
| 33.6582 | 2.9164 | ± | 0.1710 | 3.6282 |
| 34.1815 | 2.9223 | ± | 0.1733 | 3.6456 |
| 34.7026 | 2.9278 | ± | 0.1756 | 3.6625 |
| 35.2191 | 2.9338 | ± | 0.1779 | 3.6798 |
| 35.7361 | 2.9385 | ± | 0.1802 | 3.6959 |
| 36.2467 | 2.9443 | ± | 0.1824 | 3.7130 |
| 36.7555 | 2.9497 | ± | 0.1847 | 3.7295 |
| 37.2641 | 2.9540 | ± | 0.1869 | 3.7450 |
| 37.7678 | 2.9588 | ± | 0.1891 | 3.7610 |
| 38.2701 | 2.9630 | ± | 0.1914 | 3.7763 |
| 38.7801 | 2.9636 | ± | 0.1936 | 3.7882 |
| 39.2763 | 2.9680 | ± | 0.1958 | 3.8035 |
| 39.7724 | 2.9715 | ± | 0.1979 | 3.8181 |
| 40.2629 | 2.9760 | ± | 0.2001 | 3.8335 |
| 40.7561 | 2.9786 | ± | 0.2023 | 3.8470 |
| 41.2407 | 2.9833 | ± | 0.2044 | 3.8625 |
| 41.7224 | 2.9882 | ± | 0.2066 | 3.8781 |
| 42.2065 | 2.9912 | ± | 0.2087 | 3.8919 |
| 42.6876 | 2.9943 | ± | 0.2108 | 3.9058 |
| 43.1681 | 2.9968 | ± | 0.2130 | 3.9189 |
| 43.6409 | 3.0009 | ± | 0.2151 | 3.9336 |
| 44.1100 | 3.0052 | ± | 0.2172 | 3.9484 |
| 44.5820 | 3.0075 | ± | 0.2193 | 3.9613 |
| 45.0612 | 3.0065 | ± | 0.2213 | 3.9710 |
| 45.5251 | 3.0100 | ± | 0.2234 | 3.9850 |
| 45.9938 | 3.0106 | ± | 0.2255 | 3.9960 |
| 46.4545 | 3.0112 | ± | 0.2275 | 4.0070 |
| 46.8997 | 3.0165 | ± | 0.2295 | 4.0223 |
| 47.3406 | 3.0227 | ± | 0.2315 | 4.0384 |
| 47.7842 | 3.0271 | ± | 0.2335 | 4.0528 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 49.839 ± 0.005 ºC |  |  |  |  |
| 48.2406 | 3.0261 | ± | 0.2355 | 4.0622 |
| 48.6844 | 3.0290 | ± | 0.2375 | 4.0751 |
| 49.1258 | 3.0318 | ± | 0.2395 | 4.0879 |
| 49.5688 | 3.0332 | ± | 0.2415 | 4.0993 |
| 50.0081 | 3.0349 | ± | 0.2434 | 4.1110 |
| 50.4418 | 3.0378 | ± | 0.2454 | 4.1237 |
| 50.8720 | 3.0412 | ± | 0.2473 | 4.1369 |
| 51.3078 | 3.0418 | ± | 0.2493 | 4.1474 |
| 51.7431 | 3.0419 | ± | 0.2512 | 4.1573 |
| 52.1848 | 3.0384 | ± | 0.2531 | 4.1638 |
| 52.6053 | 3.0415 | ± | 0.2550 | 4.1766 |
| 53.0301 | 3.0423 | ± | 0.2569 | 4.1871 |
| 53.4566 | 3.0418 | ± | 0.2588 | 4.1963 |
| 53.8710 | 3.0452 | ± | 0.2607 | 4.2091 |
| 54.3028 | 3.0425 | ± | 0.2626 | 4.2162 |
| 54.7199 | 3.0437 | ± | 0.2644 | 4.2270 |
| 55.1212 | 3.0503 | ± | 0.2663 | 4.2428 |
| 55.5247 | 3.0555 | ± | 0.2682 | 4.2572 |
| 55.9323 | 3.0585 | ± | 0.2700 | 4.2695 |
| 56.3514 | 3.0567 | ± | 0.2719 | 4.2773 |
| 56.7590 | 3.0583 | ± | 0.2737 | 4.2883 |
| 57.1615 | 3.0612 | ± | 0.2755 | 4.3004 |
| 57.5616 | 3.0641 | ± | 0.2774 | 4.3125 |
| 57.9610 | 3.0667 | ± | 0.2792 | 4.3243 |
| 58.3700 | 3.0649 | ± | 0.2810 | 4.3320 |
| 58.7686 | 3.0664 | ± | 0.2828 | 4.3426 |
| 59.1597 | 3.0700 | ± | 0.2846 | 4.3552 |
| 59.5538 | 3.0717 | ± | 0.2864 | 4.3660 |
| 59.9403 | 3.0756 | ± | 0.2882 | 4.3788 |
| 60.3337 | 3.0761 | ± | 0.2900 | 4.3884 |
| 60.7316 | 3.0742 | ± | 0.2917 | 4.3957 |
| 61.1411 | 3.0671 | ± | 0.2935 | 4.3981 |
| 61.5213 | 3.0707 | ± | 0.2952 | 4.4104 |
| 61.9153 | 3.0687 | ± | 0.2970 | 4.4176 |
| 62.3068 | 3.0670 | ± | 0.2987 | 4.4249 |
| 62.6820 | 3.0704 | ± | 0.3005 | 4.4370 |

Online resource 9: continued.

| p | nexc (Helium) |  |  | na |
| --- | --- | --- | --- | --- |
| /(bar) | /(mmol∙g-1) |  |  | /(mmol∙g-1) |
| T = 49.839 ± 0.005 ºC |  |  |  |  |
| 63.0610 | 3.0715 | ± | 0.3022 | 4.4469 |
| 63.4399 | 3.0719 | ± | 0.3039 | 4.4562 |
| 63.8168 | 3.0698 | ± | 0.3056 | 4.4628 |
| 64.1827 | 3.0716 | ± | 0.3073 | 4.4731 |
| 64.5398 | 3.0764 | ± | 0.3090 | 4.4861 |
| 64.9005 | 3.0792 | ± | 0.3106 | 4.4974 |
| 65.2649 | 3.0802 | ± | 0.3123 | 4.5068 |
| 65.6274 | 3.0813 | ± | 0.3140 | 4.5164 |
| 65.9877 | 3.0827 | ± | 0.3156 | 4.5262 |
| 66.3427 | 3.0855 | ± | 0.3173 | 4.5373 |
| 66.6957 | 3.0884 | ± | 0.3189 | 4.5485 |
| 67.0524 | 3.0893 | ± | 0.3205 | 4.5577 |
| 67.4174 | 3.0864 | ± | 0.3222 | 4.5633 |
| 67.7657 | 3.0892 | ± | 0.3238 | 4.5743 |
| 68.1166 | 3.0904 | ± | 0.3254 | 4.5836 |
| 68.4717 | 3.0893 | ± | 0.3270 | 4.5908 |
| 68.8163 | 3.0916 | ± | 0.3286 | 4.6012 |
| 69.1581 | 3.0943 | ± | 0.3303 | 4.6119 |

Online resource 10: Dubinin-Radushkevich transformed isotherm of CO2 adsorption on zeolite 4A at 0°C (inset: linear portion from p°/p = 3.33 ∙ 10-3 – 9.58 ∙ 10-3).

(11)

(12)

.			      (13)

Online resource 14: Micropore volume and surface area calculation values

| Description | Value | Literature |
| --- | --- | --- |
| Mass of adsorbent | 0.0886 g | Measured |
| Density of adsorbed phase | 0.92743 g ∙ cm-3 | (Span and Wagner 1996) |
| Molecular cross section | 1.70 ∙ 10-19 m2 | (McClellan and Harnsberger 1967) |

Bering, B., Dubinin, M., Serpinsky, V.: Theory of volume filling for vapor adsorption. Journal of colloid

and interface science 21(4), 378-393 (1966)

Dubinin, M.: Adsorption in micropores. Journal of Colloid and Interface Science 23(4), 487-499 (1967)

McClellan, A.L., Harnsberger, H.F.: Cross-sectional areas of molecules adsorbed on solid surfaces.

Journal of Colloid and Interface Science 23(4), 577-599 (1967)

Span, R., Wagner, W.: A new equation of state for carbon dioxide covering the fluid region from the

triple‐point temperature to 1100 K at pressures up to 800 MPa. Journal of physical and chemical reference data 25(6), 1509-1596 (1996)

W is the amount of CO2 adsorbed in units of grams.